#### Continuing Education Programme (CEP) on “Advanced

Piezoelectric Materials and Devices”

Solid State Physics Laboratory (SSPL), DRDO, Delhi, September 17-19, 2025

Determination of electromechanical parameters of piezoelectric ceramics using vector impedance spectroscopy

Dr Anoop Kumar Shukla, Associate Professor, Department of Physics, Amity Institute of Applied Sciences,

Amity University Uttar Pradesh, Noida, G B Nagar. E Mail: akshukla@amity.edu

#### Contents

- Piezoelectric effect

- Vector – Impedance Characterization of a Piezoelectric Radial Mode Resonator

  - Evaluation of electromechanical parameters through equivalent circuit analysis

  - Evaluation of electromechanical parameters through direct measurement of series and parallel resonance frequencies

- Comparison of results obtained from two approaches

- Some ongoing work on lead-free materials materials in our group

- Few applications of piezoelectric materials

### Piezoelectric Effect

- Discovered in 1880 by the brothers Pierre Curie and Jacques Curie

- There are certain materials which become polarized under mechanical stress

- A potential difference is created due to mechanical stress applied in certain directions

- Piezoelectric Effect: Pressure – Electricity

- Material must be non-centrosymmetric

- Quartz, Lithium Niobate, Barium Titanate, Lead Zirconate Titanate

### Direct piezoelectric effect (Generator Action)

- Change in surface charge density due to applied mechanical

stress

- Contraction and elongation of material produce opposite charges on a particular face

- The developed polarization is directly proportional to the stress

- First order approximation

- 𝐷 = 𝑑𝑇, d is piezoelectric charge constant

- D is dielectric displacement (C/m2), T is applied stress (N/m2)

- d is charge constant (C/N)

### Mechanical to Electrical Energy Conversion

- Centrosymmetric crystals do not produce polarization under mechanical stress

- After compression or elongation, the center of symmetry does not change and hence P = 0

- Consider a non-centrosymmetric hexagonal unit cell

- F = 0, the centers of mass for positive and negative ions

coincide.

- F is applied in Y-direction centers of mass for positive and negative ions shift leading to a net dipole moment P along y.

- F is applied along X, which may not produce net dipole moment in X-direction

A

O

B

(a)

P = 0

y

A''

B''

x

P = 0

P

(c)

A'

B'

P

(b)

- The net dipole moment may be observed along Y-direction

Picture courtesy From Principles of Electronic Materials and Devices, Third Edition, S.O. Kasap (© McGraw-Hill, 2005)

### Piezoelectric Coupling Coefficients

  - The piezoelectric materials convert the mechanical energy to electrical energy

  - Application of electric field produces mechanical strain in the piezoelectric

material

  - Piezoelectric materials are electromechanical transducers

  - The	energy	conversion	in	piezoelectric	materials	is	characterized	by

piezoelectric coupling factor (k)

  - 𝑘2 = 𝑒𝑙𝑒𝑐𝑡𝑟𝑖𝑐𝑎𝑙 𝑒𝑛𝑒𝑟𝑔𝑦 𝑐𝑜𝑛𝑣𝑒𝑟𝑡𝑒𝑑 𝑡𝑜 𝑚𝑒𝑐ℎ𝑎𝑛𝑖𝑐𝑎𝑙 𝑒𝑛𝑒𝑟𝑔𝑦	or

𝑖𝑛𝑝𝑢𝑡 𝑒𝑙𝑒𝑐𝑡𝑟𝑖𝑐𝑎𝑙 𝑒𝑛𝑒𝑟𝑔𝑦

  - 𝑘2 = 𝑚𝑒𝑐ℎ𝑎𝑛𝑖𝑐𝑎𝑙 𝑒𝑛𝑒𝑟𝑔𝑦 𝑐𝑜𝑛𝑣𝑒𝑟𝑡𝑒𝑑 𝑡𝑜 𝑒𝑙𝑒𝑐𝑡𝑟𝑖𝑐𝑎𝑙 𝑒𝑛𝑒𝑟𝑔𝑦

𝑖𝑛𝑝𝑢𝑡 𝑚𝑒𝑐ℎ𝑎𝑛𝑖𝑐𝑎𝑙 𝑒𝑛𝑒𝑟𝑔𝑦

Efficiency and charge constant

The efficiency of a piezoelectric material is defined as

𝜂 = 𝑂𝑢𝑡𝑝𝑢𝑡 𝑚𝑒𝑐ℎ𝑎𝑛𝑖𝑐𝑎𝑙 𝑒𝑛𝑒𝑟𝑔𝑦Τ𝐶𝑜𝑛𝑠𝑢𝑚𝑒𝑑 𝑒𝑙𝑒𝑐𝑡𝑟𝑖𝑐𝑎𝑙 𝑒𝑛𝑒𝑟𝑔𝑦

Or

𝜂 = 𝑂𝑢𝑡𝑝𝑢𝑡 𝑒𝑙𝑒𝑐𝑡𝑟𝑖𝑐𝑎𝑙 𝑒𝑛𝑒𝑟𝑔𝑦Τ𝐶𝑜𝑛𝑠𝑢𝑚𝑒𝑑 𝑚𝑒𝑐ℎ𝑎𝑛𝑖𝑐𝑎𝑙 𝑒𝑛𝑒𝑟𝑔𝑦

- Piezoelectric Charge Constant

- The magnitude of the strain S produced by electric field E

- 𝑑 = 𝑆Τ𝐸 = 𝐷Τ𝑇

- Unit is C/N or m/V

- Important figure of merit for actuator application

Piezoelectric voltage constant

    - The induced electric field E in the material is related to the applied stress T

    - Parameter relating E and T is known as piezoelectric

voltage constant (g)

    - The voltage constant is defined as 𝑔 =	𝑑

𝗌𝑜𝗌𝑟

    - The piezoelectric voltage constant is important figure of merit for electromechanical sensor applications and piezoelectric energy harvesting devices

### Converse Piezoelectric Effect (Motor Action)

V=0

A mechanical strain is observed under application of an

electric field

- Material	exhibit	expansion	or	contraction	depending upon the direction of the electric field

- The strain is directly proportional to the applied field

- 𝑆 = 𝑑𝐸

- d is piezoelectric charge constant (m/V)

V0

- 𝑑 =

𝑆Τ𝐸 =

𝐷Τ𝑇same for both direct and converse effects

### Piezoelectric constitutive equations

#### In	piezoelectric	effect,	the	elastic	variables	(T	and	S)are	related	to	the electrical variable (D and E)

  - The constitutive equations for direct and converse piezoelectric effects can be expressed as

  - 𝑫 = 𝒅𝑻 + 𝜺𝑻𝑬, here 𝜺𝑻is the permittivity under constant stress (usually zero)

  - 𝑺 = 𝒔𝑬𝑻 + 𝒅𝑬, here 𝒔𝑬is the elastic compliance under constant electric field (usually zero)

### Polarization and electric displacement tensors

- Piezoelectric effect is observed in anisotropic dielectrics

- Hence 𝑃 = 𝜒𝜀𝑜𝐸 and 𝐷 = 𝜀𝐸 should be replaced by tensors

𝑷𝟏 = 𝝌𝟏𝟏𝜺𝒐𝑬𝟏 + 𝝌𝟏𝟐𝜺𝒐𝑬𝟐 + 𝝌𝟏𝟑𝜺𝒐𝑬𝟑

𝑷𝟐 = 𝝌𝟐𝟏𝜺𝒐𝑬𝟏 + 𝝌𝟐𝟐𝜺𝒐𝑬𝟐 + 𝝌𝟐𝟑𝜺𝒐𝑬𝟑

𝑷𝟑 = 𝝌𝟑𝟏𝜺𝒐𝑬𝟏 + 𝝌𝟑𝟐𝜺𝒐𝑬𝟐 + 𝝌𝟑𝟑𝜺𝒐𝑬𝟑

𝑫𝟏 = 𝜺𝟏𝟏𝑬𝟏 + 𝜺𝟏𝟐𝑬𝟐 + 𝜺𝟏𝟑𝑬𝟑

𝑫𝟐 = 𝜺𝟐𝟏𝑬𝟏 + 𝜺𝟐𝟐𝑬𝟐 + 𝜺𝟐𝟑𝑬𝟑

𝑫𝟑 = 𝜺𝟑𝟏𝑬𝟏 + 𝜺𝟑𝟐𝑬𝟐 + 𝜺𝟑𝟑𝑬𝟑

- Since𝜒𝑖𝑗 = 𝜒𝑗𝑖 and 𝜀𝑖𝑗 = 𝜀𝑗𝑖

- Number of independent electrical coefficients are six

Piezoelectric Coefficient tensor

- Application of a mechanical stress T produces a strain S and

Z	3

6

5

2

Y

electrical polarization P

- Similarly application of an electric field E causes an electric polarization P and strain S

- 𝑃𝑖 = σ𝑗 𝑑𝑖𝑗𝑇𝑗, 𝑆𝑖𝑗 = σ𝑖 𝑑𝑖𝑗𝐸𝑖, (i = 1,2,3, j=1,2,3,4,5,6)

- A	piezoelectric	material	can	be	described	by	a	matrix	of

electromechanical coefficient

- Piezoelectric coefficients, elastic constants, and permittivity are	1

all tensors	X	4

- Permittivity- Second Rank, Piezoelectric Coefficient-Third Rank

and Elastic compliance-Fourth Rank tensors

- Axes notation, Cartesian System X-, Y- and Z- are 1, 2 and 3

- The shear effects are represented as 4, 5 and 6

#### Vector Impedance Characterization of a Piezoelectric Ceramic Resonator

Impedance/Admittance-Phase measurement

Material: Pb(Zr0.57, Ti0.43)O3 + 6 at % of lanthanum

##### Characteristic frequencies of a piezoelectric resonator

Frequencies fm & fn corresponds to minimum and maximum impedance

Frequencies at which reactance Xe = 0, are the resonant and anti-resonant frequencies fr & fa

##### Evaluation of electromechanical parameters using equivalent circuit analysis

Equivalent circuit of a piezoelectric resonator

Cb

R

R

G	  1

L	b

b

Ca

R – Motional resistance	L – Motional inductance

Rb – Shunt resistance

Ca– Motional capacitance

Cb– Shunt capacitance

Simulated values of piezoelectric equivalent circuit parameters R, L, Ca, Cb and Rb

for fundamental radial mode and its overtone

| x (at% of La) | Rb infinite |  |  |  | Rb finite |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | R (ohm) | L (mH) | Ca (pF) | Cb (nF) | R (ohm) | L (mH) | Ca (pF) | Cb (nF) | Rb (ohm) |
| 3.0 | 49.5 147.5 223.2 | 5.32 5.75 5.10 | 217.7 29.5 13.7 | 0.796 0.754 0.776 | 49.4 145.0 217.7 | 5.32 5.84 5.47 | 217.7 29.1 12.8 | 0.796 0.749 0.770 |  37.2103 7.0103 |
| 5.0 | 24.5 77.0 120.6 | 2.48 2.49 2.22 | 490.1 72.4 33.6 | 1.389 1.293 1.326 | 24.5 74.4 118.3 | 2.48 2.55 2.37 | 490.1 70.73 31.4 | 1.389 1.277 1.309 |  13.2103 4.4103 |
| 6.0 | 20.2 71.6 121.4 | 1.73 1.85 1.67 | 708.3 98.9 45.4 | 1.906 1.766 1.815 | 20.2 70.2 120.5 | 1.73 1.90 1.91 | 708.3 96.7 39.7 | 1.906 1.748 1.788 |  11.6103 2.0103 |
| 8.0 | 17.8 86.7 141.7 | 1.52 2.00 1.62 | 657.0 75.2 38.1 | 2.203 2.117 2.329 | 17.8 85.8 144.6 | 1.52 2.06 2.16 | 657.0 72.9 28.6 | 2.203 2.097 2.268 |  7.4103 1.2103 |
| 10.1 | 57.9 166.0 281.8 | 4.68 4.54 3.15 | 277.6 42.8 25.1 | 2.006 1.999 2.071 | 57.9 162.0 275.7 | 4.68 5.09 5.22 | 277.6 38.2 15.1 | 2.006 1.971 2.055 |  3.3103 1.3103 |
| 12.1 | 28.0 94.7 175.8 | 2.58 2.59 1.95 | 321.7 48.5 26.3 | 2.112 2.127 2.219 | 28.0 92.0 176.0 | 2.58 2.80 2.93 | 321.7 44.8 17.1 | 2.112 2.097 2.233 |  2.9103 0.9103 |

##### Significance of equivalent circuit parameters

- R represents mechanical dissipation of the piezoelectric resonator.

- L represents mass transformed into electrical magnitude by piezoelectric effect.

- Ca represents elastic compliance transformed into electrical magnitude by piezoelectric effect.

- Cb	is the capacitance in the absence of mechanical deformations at the concerned frequency of

resonance

- Rb is the loss associated with Cb

- In general, these parameters are independent of frequency

- This is true only for a narrow range of frequencies near the resonance frequency

##### Determination of electromechanical parameters according to IEEE std.

For Gb→0 the impedance of this circuit is given

ω

ωsQmR

jω r

1 + jQm

ωൗω

s

−

ωsൗω

1 + jQ

m

1 + r ൗ

r

ωൗ

ωp

−

ωpൗ

ω

Cb

Z	=

=  Z ∠θ

= Re + jXe

a

Capacitive ratio r = CbൗC

R

R

G	  1

QmΤr

M =

= 1Τ

L	b

b

1Τ L.Ca

ωsCbR

ωs = 2π fs =

1 +  1Τr

Ca

ωp = 2π fp = ωs

(Proc. IRE 45, 354(1957))

##### Determination of electromechanical parameters according to IEEE std.

- The planar coupling coefficient KP can be determined

J1 φ 1+ Δfൗfs

−φ 1+ Δfൗfs

J1 φ 1+ Δfൗfs

J0 φ 1+ Δfൗfs

1−σE

P

K2

1+σE

P

1−K2 =

- Here ∆fps =fp-fs. J0 & J1 are the Bessel function of first kind and zero order and first order

- E is the Poisson’s ratio

1 − σE

φ is the lowest positive root of the equation

J1

= φJ0

φ

φ

The roots of this equation are related the resonant frequencies of fundamental and overtones of

radial mode of the thin circular discs.

1 − σE

K

2	2

31

P

The coupling coefficient K31 can be determined as K	= 0.5

(Proc. IRE 49, 1161(1961))

##### Determination of electromechanical parameters according to IEEE std.

  - The elastic compliance can be calculated from

s

1	4π2a2f 2 1 − σE2	ρ

s

E	=	φ2

11

  - Here ‘a’ is the radius of the disk and ‘’ is the density of the material

  - The piezoelectric strain constant d31

= K31

1Τ2

ε0εT

33 11

sE

Hydrostatic piezoelectric strain constant dh = d33 + 2d31

  - Piezoelectric voltage constants g31 =

d31Τε0εT	, g33 =

d33Τε0εT

33

33

s

E

Acoustical velocity V2 = 1Τ

11	ρ

1 − σE2

33

31

Here 𝜀𝑇	is the dielectric constant and d

is negative

#### Calculation of Poisson’s ratio

- Poisson’s ratio can be calculated from the ratio of resonance frequencies of fundamental and first overtone

sE

12	11

ൗsE

1 − σE

σE = −

J1

3

φ

φ

= φJ0

2

φiV

1	2

2 1Τ2	1

1− 1Τ3	φ σ tൗ 1−σ	2a

i

E

E

2

1− 1Τ3	φ σ tΤ 1−σ	2a

0

E

E

2

ωφi =

a	1 − 3 γiφi

, Where γi=1 for all ’s.	0

•

2

ωsi ωs0

φiΤφ0

=

2

σEt

1−σE 2a

-1

-2

-3

0	2	4	6	8	10	12

Evaluation of electromechanical parameters through

direct measurement of fs and fp

#### Direct measurement of fs, fp and calculation of electromechanical parameters

𝑌 𝜔

At the series resonant frequency fs, real part of	𝜔	is maximum

𝜔

At parallel resonant frequency fp, the real part of ωZ

is maximum

S. Sherrit, N. Gautheir, H. D. Wiederick and B. K. Mukherjee, Ferroelectrics. 119, 17 (1991).

#### Direct measurement of fs, fp and calculation of electromechanical parameters

- The admittance of radial resonator is given as

- 𝑌

−jω ε0𝗌𝑝	πa2

𝜔

33

=

𝑡

− 1 ,	𝐽

= xJ0 𝑥

𝑥

𝐽1 𝑥

,	𝑥 =	ωa

2 𝑘𝑝 2

1−𝜎𝑝−𝐽 ωaൗ 𝑐𝑝

1Τ2

11

ൗ𝜌

𝑐𝑝

11

ൗ𝜌

Once the 𝜎𝑝 and p are known 𝑘𝑝 can be determined from

𝑘𝑝

1−𝜎𝑝−𝐽 𝜔 𝑎ൗ 𝑐𝑝

𝑝

11

1Τ2

ൗ𝜌

2 =

2

IEEE Standards on Piezoelectricity, 176 (1978).

#### Direct measurement of fs, fp and calculation of electromechanical parameters

- Knowing fs

and fp

of the fundamental and first harmonic 𝜎𝑝and 𝑐𝑝	can be determined by the non-linear

11

least square polynomial fits of the equations

𝑠

𝑟

𝑠

𝜂 = 𝑎0 + 𝑎1𝑟𝑠 + 𝑎2𝑟2 + 𝑎3	3

2

𝑠

0

𝜎𝑝 = 𝑏0 + 𝑏1𝑟𝑠 + 𝑏

𝑟2 + 𝑏

𝑟3 + 𝑏

𝑟4

𝜌Τ𝑐𝑝

11

3

𝑠

4

𝑠

1

The coefficients {an, bn} are taken from Table I of Sherrit et al. [7] and rs is defined as 𝑟𝑠 =

𝑓𝑠

ൗ𝑓𝑠

- 𝜂 can be evaluated from 𝜂 = 2π f𝑠

0 𝑎

1Τ2

#### Direct measurement of fs, fp and calculation of electromechanical parameters

  - Poisson’s ratio 𝜎𝑝, radial mode coupling coefficient 𝑘𝑝, piezoelectric constant 𝑒𝑝	, dielectric constant 𝜀𝑝	and

31	33

11

and mechanical constants 𝑐𝑝	are defined as

  - 𝜎𝑝 =

−𝑠𝐸

ൗ𝑠𝐸	, 𝜀𝑝

2

𝑠𝐸

11	12

+𝑠𝐸

2d

= 𝜀′ −	31	, 𝑐𝑝

𝐸

𝑠𝐸

11

𝑠𝐸

12

𝑠

=	11	,

12	11

33

𝗌0

11	2−	2

  - 𝑒𝑝	=	𝑑31

,

𝑝	2

𝑘𝑝

2 =	𝑒31	,

31	𝑠𝐸	+𝑠𝐸

𝗌0𝗌𝑝	𝑐𝑝

11	12

33 11

  - The planar coupling coefficient KP as defined earlier is related to radial mode coupling coefficient kp as

𝑘𝑝

2 = 1+𝜎𝑝

2

𝐾2

𝑃

𝑃

,

1−𝐾2

IEEE Standards on Piezoelectricity, 176 (1978).

##### Comparison of results obtained from two approaches

- Pb(Zr

Ti	)O

+ x at % of La,

| x (at% of La) | fs(kHz) |  | fp(kHz) |  |
| --- | --- | --- | --- | --- |
|  | observed | calculated | observed | calculated |
| 3.0 | 147.80 386.45 602.79 | 147.83 386.41 602.78 | 166.79 393.89 608.03 | 166.82 393.90 608.07 |
| 5.0 | 144.32 374.65 583.46 | 144.24 374.66 583.45 | 167.85 384.71 591.03 | 167.77 385.00 590.79 |
| 6.0 | 143.68 371.82 578.79 | 143.67 371.80 578.49 | 168.25 381.90 585.52 | 168.26 382.01 585.68 |
| 8.0 | 159.08 410.56 640.61 | 159.03 410.45 640.05 | 181.17 417.59 645.05 | 181.20 417.68 645.26 |
| 10.1 | 139.67 361.28 566.76 | 139.64 361.06 565.96 | 148.97 364.95 569.22 | 148.99 364.91 569.38 |
| 12.1 | 174.58 449.48 703.92 | 174.74 449.26 703.46 | 187.63 454.31 706.68 | 187.58 454.36 707.61 |

0.57,	0.43	3

where x = 3, 5, 6, 8, 10 and 12

- Close agreement between two approaches, and either of the methods are valid for low loss piezoelectric materials

- For lossy piezoelectric materials, e.g. ceramic polymer composites one should consider the constants as complex parameters

Shukla et al(2004): Ferroelectrics, 308:1, 67-84

sεdKEpppp0

σfecεk11s33121311P

##### Comparison of results obtained from two approaches

Equivalent circuit analysis	Direct measurement of fs and fp

| x (at% of La) | 𝜎𝐄 | 𝐾𝑃 | 𝑠𝐸 11 10-12 m2/N | 𝑑31 10-12 C/N |
| --- | --- | --- | --- | --- |
| 3.0 | 0.31 | 0.52 | 14.1 | -100 |
| 5.0 | 0.32 | 0.58 | 15.9 | -157 |
| 6.0 | 0.34 | 0.59 | 16.7 | -197 |
| 8.0 | 0.33 | 0.54 | 14.7 | -182 |
| 10.1 | 0.33 | 0.39 | 18.3 | -129 |
| 12.1 | 0.35 | 0.41 | 12.5 | -115 |

| x (at% of La) | 𝜎𝑝 | 𝐾𝑃 | 𝑠𝐸 11 10-12 m2/N | 𝑑31 10-12 C/N |
| --- | --- | --- | --- | --- |
| 3.0 | 0.32 | 0.52 | 14.25 | -96 |
| 5.0 | 0.35 | 0.58 | 16.58 | -154 |
| 6.0 | 0.36 | 0.59 | 17.14 | -192 |
| 8.0 | 0.37 | 0.54 | 15.25 | -178 |
| 10.1 | 0.36 | 0.39 | 19.02 | -118 |
| 12.1 | 0.38 | 0.42 | 12.91 | -114 |

##### Development of doped barium zirconate titanate (BZT) based piezoelectric ceramics for acoustic emission sensor applications

Developed for DMRL, Hyderabad, supplied ~400g powder and ~20 sintered discs with density >95%

##### Piezoelectric response of Cd-doped BCZT ceramics

| Sintering temperature (oC) | Cd content (x) | kp | kt | d33 (pC/N) |
| --- | --- | --- | --- | --- |
| 1400 | 0.00 | 0.32 | 0.30 | 311 |
|  | 0.02 | 0.46 | 0.44 | 420 |
|  | 0.04 | 0.19 | 0.18 | 178 |
|  | 0.06 | 0.14 | 0.14 | 176 |
|  | 0.00 | 0.40 | 0.39 | 404 |
| 1450 | 0.02 | 0.18 | 0.18 | 200 |
|  | 0.04 | 0.16 | 0.16 | 165 |
|  | 0.06 | 0.13 | 0.12 | 104 |
|  | 0.00 | 0.46 | 0.44 | 500 |
| 1500 | 0.02 | 0.17 | 0.16 | 175 |
|  | 0.04 | 0.16 | 0.16 | 135 |
|  | 0.06 | 0.10 | 0.09 | 98 |

Salma et al. Ceramics International 51 (2025) 41251–41263

Applications of Piezoelectric Materials

#### Applications of Piezoelectric Materials

Generators

(millivolts to kilovolts)

Motors

(microns to millimeters)

- Hydrophones

- Microphones

- Gas igniters

- Accelerometer

- Power supplies

- Photoflash actuators

- Piezoelectric pens

- Impact fuses

- Composites

- Energy harvesting

- Actuators

- Loudspeakers

- Camera shutters

- Buzzers

- Ink jet printers

- Fish finders

- Micropositioners

- Valve controllers

- Pumps

- Video head positioner

- Ultrasonic motors

- Piezoelectric fans

- Relays

## Applications contd.

Motor – Generator

(combination devices)

  - Sonar

  - Non – destructive testing (NDT)

  - Medical ultrasound

Resonant devices

(kilohertz to megahertz)

- Ultrasonic cleaners

- Ultrasonic welders

- Filters

- Transformers

# Piezoelectric Gas Igniter

- A piezoelectric crystal is the heart of the gas igniter.

- When a strong force is applied on it by means of a spring loaded hammer it produces an electric spark.

- Requires no batteries or fuel

Piezoelectric Actuators

  - Displacement of up to several hundreds of microns with high

accuracy (  0.01 µm)

  - High Response time on the order of 10 µs.

  - Generative force as large as 400 kg/cm2

  - Driving	power	an	order	of	magnitude	smaller	than electromagnetic motors

In Space Structure and Military Vehicles Using P/E Actuators

Automation

Equipment

Optical Instrument.

Camera

Semi-conductive Chips

VIBRATION SUPPRESSORS

MOTORS

POSITIONER

ACTUATORS APPLICATION FIELDS

# Piezoelectric Motor

SQUIGGLE* Linear Piezoelectric Motor

only 1.55x1.55x6 millimeters

Uses  less  than

0.1    Watt    to

produce 20 grams of force at 5 mm per second.

*Registered trademark of New Scale Technologies, Inc., USA

Auto focusing in camera installed cell phones

Flexure guide

Retracted Lens

Motor

Extended Lens

Courtesy New Scale Technologies, Inc., USA

Piezoelectric Biosensors

- Blood, urine and saliva analysis

- HIV, Anthrex and Hepatitis detection

- Lab on a chip

- Work is in preliminary stage at international level

## Schematic diagram of a piezoelectric biosensor

Piezoelectric crystal

Courtesy www.biomed.drexler.edu/technologyportfolio

## Acoustic Emission Sensor

- Acoustic Emission (AE) can be defined as the vibration or stress waves generated during dynamic process in materials.

- AE monitoring system consists basically of a detector or pick-up to detect the material’s noise vibration and convert it to an equivalent electrical signal.

# Ultrasound Imaging

- After	X-rays,	the	ultrasound	imaging	is	most	extensively	used	technique	in biomedical field.

- The ultrasound is a safe, real time, accurate, reliable, portable and cost effective imaging technique.

- It is used for characterizing the heart function, monitoring the growth of fetus in womb, locate cyst in liver / kidney, and assess carotid plaques and breast tumor

- Ultrasound imaging is less hazardous to soft tissues

# Ultrasound imaging

Receiver

Transmitter

Control

Acoustic matching layer

Acoustic lens

Object

Transducer: PZT, PMN-PT, PZNT,PVDF

– TrFE etc

Scan Frame

Coupling layer

A K Shukla, S L Srivastava, Smart Materials : Piezoelectrics, Nova Science Publisher, USA, 2012

# Ultrasound Imaging

  - The ultrasound imaging uses pulse echo technique for imaging of the biological organs.

  - The piezoelectric materials generate and sense the acoustical signals and, therefore, suited for pulse echo measurements.

  - The piezoelectric transducer sends the ultrasonic pulse which senses the echoes also from the various obstacles in the path.

# Energy Harvesting

- The search for environment friendly alternative energy sources is need of the day to overcome future energy problems.

- Extraction of energy from the external sources of environment (solar power, thermal energy, wind energy, salinity gradients, and kinetic energy), and storage for further utilization.

# Piezoelectric Energy Harvesting

Capacitor

bank

Piezoelectric

device

Voltage sensing switch

Operating sensor/actuator, telemetry, MEMS etc

Strain

energy

The vibrating strain energy is converted in the electrical energy using a piezoelectric system.

  - This energy is stored using a rectifier into a capacitor bank up to a pre defined voltage.

  - Exceeding this voltage, the power is

transferred to the load.

# Piezoelectric Energy Harvesting

#### Acknowledgements

- DDP, DST; ARDB, and ER&IPR, DRDO for grant of research projects

- Amity University for providing necessary facilities

- Late Dr. A R James, SC’G’, DMRL, Hyderabad for VIS measurement for ARDB, DRDO

project

- Prof. K Sreenivas, University of Delhi, and Dr. O P Thakur, SC’G’, SSPL, New Delhi for many

useful scientific discussions and support

THANK YOU